## Slide 1: Understanding spin-orbit torque domain wall logic devices
15 nm
3 nm
3 nm
HM
CoFeB

## Slide 2
To reduce the DW depinning current, pin the DW on edge roughness
The DW settles to a band of positions for a given pulse width due to geometry variations, a longer track is needed to separate the states
120nm track
3×1010 A/m2, 2 ns pulse
2 ns pulse
6 ns pulse
320nm track
3×1010 A/m2, 6 ns pulse

## Slide 3
DW can be reliably driven back and forth with opposite polarity pulses
5 ns
5 ns
(+) pulse
(+) & (–) pulse

## Slide 4
(+) pulse
(+) & (–) pulse
Strong reset is important regardless of device state
State after input high
State after reset
Jhigh
Jlow
State after input low, before reset
MTJ

## Slide 5
Inertia?
5 ns
5 ns
5 ns
5 ns

## Slide 6
V
RMTJ
J2 (t) =
Jhigh if x(t) > xR
Jhigh / (1 + TMR) if x(t) < xL
Jhigh
x1(t) – xL
xR – xL
+
xR – x1(t)
xR – xL
if xL < x(t) < xR
1
Jhigh
1 + TMR
–1
J1
J2
An approximate model of concatenation
J1 does not vary across the track and is independent of MTJ state
J2 does not affect DW

## Slide 7
DW 1 reset
(constant J1)
Current into DW 2

## Slide 8
Time-varying current input
Jhigh = 3.0×1010
Jlow = 1.2×1010
Jhigh = 3.0×1010
Jlow = 1.0×1010
Jhigh = 3.9×1010
Jlow = 1.3×1010
(TMR = 150%)
(TMR = 200%)
(TMR = 200%)
DW 2

## Slide 9
DW1 resets later
DW2 switches first
The current input is large enough to move the DW at a moderate speed in the fat region

## Slide 11
Other more obvious solutions (that don’t work)
Higher current to give DW 2 more speed
  But DW 1 will move back faster, shortening the current pulse
Move MTJ to the left
  DW 2 will clear the MTJ faster, but DW 1 will also be reset faster
  Both DWs need to clear the MTJ with a large margin
Make second device narrower: limits cascade-ability
Are we under-estimating inertia? Is the amount of roughness too great?
The problem gets worse if we realistically model current division in the first device

## Slide 12: Metal strip on the right side of track
DW1 resets later
DW2 switches first

## Slide 13: First shot – reduces current density in region by 25%

## Slide 14: Second shot – reduces current density in region by 30%

## Slide 15: Third shot – reduces current density in region by 30%, anisotropy variation reduced

## Slide 16: Potential idea for device: VCMA pinning
J
Vpin
Use voltage- controlled pinning sites at ends of track, turn off when pulse is delivered, turn on when pulse ends

## Slide 17: To-do
Figure out geometry
Calculate electric field (electrostatics/Poisson)
Mumax3 simulations